### CHAPTER 12 | Solids: Structures and Applications

12.1. Collect and Organize

From the drawings shown in Figure P12.1, we are to choose which represents a crystalline solid and which represents an amorphous solid.

# Analyze

In crystalline solids, atoms or molecules arrange themselves in regular, repeating three-dimensional patterns. In an amorphous solid, the atoms or molecules are arranged randomly, with no defined repeating pattern.

# Solve

Drawings (b) and (d) are analogous to crystalline solids because they show a definite pattern while (a) and (c) are amorphous.

# Think About It

In drawings (b) and (d) there are two kinds of atoms; if the drawings represent metals, these two substances would be alloys.

12.2. Collect and Organize

For each of two patterns in Figure P12.2 we are to determine the unit cell and the numbers of light and dark squares within the unit cell.

# Analyze

A unit cell is the smallest repeating pattern in a two- or three-dimensional pattern.

# Solve

(a)	(b)

(a)	There are 8 light squares and one dark square in this unit cell.

(b)	There are 2 light squares (4   and 2 dark squares (4  + 1) in this unit cell.

# Think About It

Both of these unit cells are based on a square.

12.3. Collect and Organize

Using Figure P12.3, we are to determine the unit cell and write the chemical formula for the compound where element A is represented as red spheres and element B is represented as blue spheres.

# Analyze

Once the unit cell is determined, the chemical formula can be deduced. Spheres on the corner are shared by eight unit cells and so are counted as  in the unit cell. Likewise, spheres on the edges are shared by four unit cells and are counted as  in the unit cell, and spheres on the faces of the unit cell are shared by two unit cells and are counted as  in the unit cell. Any atom completely inside a unit cell belongs entirely to it and counts as 1.

# Solve

There are 8 + 6 = 4 red spheres or 4 A atoms in the unit cell. There are 12 + 1(1) = 4 blue spheres or 4 B atoms in the unit cell. The chemical formula is A4B4 or AB.

# Think About It

The empirical formula for this compound would be AB because that is the lowest whole-number ratio of elements in the substance.

12.4. Collect and Organize

Using Figure P12.4, we are to determine the number of A cations, B cations, and X anions in the portion of the unit cell shown.

# Analyze

Figure P12.4 shows 8 A cations at the corners of the cube, 6 B cations at the faces, and 1 X anions in the center. Each corner ion is shared between 8 unit cells and each face ion is shared between 2 unit cells.

# Solve

Because 8 A ions occupy the corners, and because the portion of the unit cell contains  of each corner ion, the number of A cations in the unit cell are

8 A cations  = 1 A cation in the unit cell

Because 6 B ions occupy the faces, and because the portion of the unit cell contains  of each face ion, the number of B cations in the unit cell are

6 B cations  = 3 B cations in the unit cell

Because 1 X ions occupy the center, and because the unit cell contains 1 of each center ion, the number of X anions in the unit cell is

1 X anions  1 = 1 X anion in the unit cell

This gives a total of one anion and four cations per unit cell.

# Think About It

Based on the stoichiometry in the unit cell, the formula unit for this ionic solid must be AB3X.

12.5.  Collect and Organize

We are to determine the formula of a compound in which A ions form an fcc unit cell and where half of the octahedral holes are occupied by B and one-eighth of the tetrahedral holes are occupied by C.

# Analyze

In a face-centered cubic (cubic closest-packed) array of A ions, there are 8 tetrahedral holes and 4 octahedral holes.

# Solve

The number of A ions in the fcc unit cell is

If one-half of the octahedral holes contain B ions, then there are 2 B ions in the unit cell. If one-eighth of the tetrahedral holes contain C ions, then there is 1 C ion in the unit cell. The chemical formula for this compound is A4B2C.

# Think About It

We may assume that the lattice is formed from an anion (the larger A spheres), and both species occupying the holes of the ccp lattice (the smaller B and C spheres) are cations.

12.6.  Collect and Organize

We are to determine the formula of a copper–chloride compound in which the chloride ions form an fcc arrangement and the copper ions occupy half of the tetrahedral holes.

# Analyze

In an fcc arrangement, there are 8 tetrahedral holes in the unit cell.

# Solve

The number of chloride ions in the unit cell is

The number of copper ions in the unit cell is

The formula for the compound is CuCl.

# Think About It

There are equal numbers of copper and chloride atoms in the unit cell.

12.7.  Collect and Organize

We are to determine the formula of a lithium–sulfur compound in which the sulfide ions form an fcc arrangement and the lithium ions occupy all of the tetrahedral holes.

# Analyze

In an fcc arrangement, there are 8 tetrahedral holes in the unit cell.

# Solve

The number of sulfide anions in the unit cell is

The number of lithium cations in the unit cell is 8. The formula for the compound is Li2S.

# Think About It

This salt is neutral because the charge on two lithium ions (1+) in the formula balances the charge on one sulfide anion (2–).

12.8.  Collect and Organize

From the unit cell of CsCl where the edge length is 412 pm, we are to calculate the radius of Cs+ ions knowing that the Cl– ion radius is 181 pm.

# Analyze

CsCl forms a body-centered cubic unit cell where, although the Cl– ions at the corners are not touching, the ions along the body diagonal (Cl–—Cs+—Cl–) do touch. The length of the body diagonal of the bcc unit cell is .

# Solve

Along the body diagonal we have  where r is the radius of the respective ions. Setting this equal to the length of the body diagonal and substituting in  (the unit cell edge length) and the radius of the Cl– ion gives

# Think About It

The Cs+ ion size in Figure 10.2 is 170 pm, which is close to the value calculated here. Remember that ionic size varies depending on how the ions pack in the crystals.

12.9.  Collect and Organize

We are to identify the elements highlighted in the periodic table in Figure P12.15 that do not adopt a rock salt structure for their chloride salt.

# Analyze

In the rock salt structure, the cations must fit into the octahedral holes between the closest-packed layers of Cl–. The radius ratio of cation to anion should be between 0.41 and 0.73. The radii of the cations of the highlighted elements from Figure 10.2 are Li+ (76 pm), Na+ (102 pm), K+ (138 pm), Cs+ (170 pm), and Sr2+ (118 pm). The radius of Cl– is 181 pm.

# Solve

For LiCl, the radius ratio is

For NaCl, the radius ratio is

For KCl, the radius ratio is

For CsCl, the radius ratio is

For SrCl2, the radius ratio is

By the radius ratio rule, the rock salt structure is not probable for KCl (K+ would occupy cubic holes) nor for CsCl (Cs+ would occupy cubic holes) or SrCl2 (because it does not have a 1:1 cation-to-anion stoichiometry). LiCl is borderline. In nature, all of these adopt a rock salt structure except Cs (blue) and Sr (purple).

# Think About It

In the hypothetical rock salt structure of SrCl2, Sr2+ would occupy one-half of the octahedral holes. In nature, this ionic compound instead adopts a fluorite structure.

12.10. Collect and Organize

We are to identify the elements highlighted in the periodic table in Figure P12.16 that do not adopt a fluorite (CaF2) structure.

# Analyze

The radius ratio for the tetrahedral holes in fluorite is between 0.22 and 0.41. The radii of the highlighted cations are Cs+ (170 pm), Mg2+ (72 pm), Ca2+ (100 pm), Sr2+ (118 pm), and Ba2+ (135 pm). The radius of F– is 133 pm. Because the fluoride ions might occupy the tetrahedral holes in CsF, the appropriate radius ratio for that salt is

# Solve

For CsF, the radius ratio is

For MgF2, the radius ratio is

For CaF2, the radius ratio is

For SrF2, the radius ratio is

For BaF2, the radius ratio is

The fluorite structure is not possible for any of these salts as predicted by the radius ratio rule. However, both CaF2 and SrF2 adopt the fluorite structure. The elements Cs (red), Mg (orange), and Ba (purple) do not.

# Think About It

In order for CaF2 and SrF2 to adopt the fluorite structure, the fcc arrangement of F– anions must be expanded to accommodate the relatively large Ca2+ and Sr2+ ions.

12.11. Collect and Organize

From Figure P12.11 showing the unit cell of magnesium boride, we are to determine its formula.

# Analyze

We are given that one B atom is inside the trigonal prismatic unit cell. Each corner of the unit cell has an Mg atom. Because the unit cell is trigonal prismatic, each corner atom is shared with 11 other unit cells and so has one-twelfth of its volume inside the unit cell.

# Solve

The number of B atoms in the unit cell is 1. The number of Mg atoms in the unit cell is 6 = . The formula from the unit cell is MgB2 (in the lowest whole-number ratio).

# Think About It

It is tricky to see that the Mg atoms here are shared between 12 unit cells. Consider the center atom in the figure on the right hand side. That atom is shared with 6 unit cells as shown, but there are also 6 more unit cells stacked on top of it that are not shown in the diagram.

12.12. Collect and Organize

From the diagram in Figure P12.12 showing the unit cell for a Y—Ba— Cu oxide, we are to determine the molecular formula and then consider which eight oxygens should be removed to give the unit cell for YBa2Cu3O7. We are asked whether it makes a difference which oxygen atoms are removed.

# Analyze

Atoms on the corners of the unit cell contribute of their volume to the unit cell. Atoms on the unit cell edges contribute of their volume to the unit cell. Atoms on the face of a unit cell contribute of their volume to the unit cell. Atoms inside the unit cell contribute all of their volume to the unit cell. When removing 8 oxygen atoms from the figure to give YBa2Cu3O7 we have to remove the atoms so as to maintain the stoichiometry of the superconductor.

# Solve

It does matter which oxygen atoms are removed from the structure in Figure P12.12. To obtain a formula of YBa2Cu3O7 from YBa2Cu3O9 by removing 8 oxygen atoms from the unit cell, we would have to remove the equivalent of 2 oxygen atoms. We could do this by removing 8 edge O atoms. If we removed face atoms we would only remove 4 O atoms. If we removed some edge atoms we could remove 4 edge O atoms and 2 face O atoms to obtain the correct stoichiometry.

# Think About It

The actual unit cell of the superconductor (Figure 12.34) indeed shows that removal of 8 edge O atoms gives YBa2Cu3O7.

12.13. Collect and Organize

We are asked to differentiate between cubic closest-packed (ccp) and hexagonal closest-packed (hcp) structures.

# Analyze

Both structures contain layers of close-packed atoms and differ only in how the layers are stacked.

# Solve

Cubic closest-packed structures have an abcabc… pattern, and hexagonal closest-packed structures have an abab… pattern.

# Think About It

The unit cell for ccp is face-centered cubic (Figure 12.11), and the unit cell for hcp is hexagonal (Figure 12.5).

12.14. Collect and Organize

We are asked to describe the defining features of simple cubic, body-centered cubic, and face-centered cubic crystal structures, and to rank these in order of decreasing packing efficiency.

# Analyze

Packing efficiency is a measure of the volume of the cube occupied by the atoms. The greater the volume of the cube occupied by atoms, the higher the packing efficiency.

# Solve

Simple cubic cells feature a repeating arrangement of square-packed layers directly over one another, in the pattern aaa… Overall, there is one particle contained in the volume of the unit cell, and the packing efficiency is 52%.

Body-centered cubic cells feature a repeating arrangement of square-packed layers offset with respect to each other, in the pattern ababab… Overall, there are two particles contained in the volume of the unit cell, and the packing efficiency is 68%.

Face-centered cubic cells feature a repeating arrangement of close-packed layers, staggered such that the repeating pattern is abcabc… Overall, there are four particles contained in the volume of the unit cell, and the packing efficiency is 74%.

The unit cells, in order of decreasing packing efficiency are:

face-centered cubic > body-centered cubic > simple cubic

# Think About It

Close packed layers are much more efficient at packing than square packed layers; as a result, the fcc and hcp structures have a higher packing efficiency than simple cubic and bcc.

12.15. Collect and Organize

We are asked which has the greater packing efficiency, the simple cubic or the body-centered cubic structure.

# Analyze

Packing efficiency is the fraction of space within a unit cell that is occupied by the atoms.

# Solve

We read in Section 12.2 of the textbook that the simple cubic cell has the lowest packing efficiency of all the unit cells, so the body-centered cubic structure has a greater packing efficiency than the simple cubic structure.

# Think About It

The packing efficiency of the unit cell structures can be calculated. For simple cubic, the packing efficiency is only 52%, whereas for body-centered cubic it is 68% and for face-centered and hexagonal it is 74%.

12.16. Collect and Organize

By looking at Figure 12.10 we are to predict which structure, body-centered cubic (bcc) or face-centered cubic (fcc), has the greater packing efficiency.

# Analyze

In the face-centered cubic unit cell, there are atoms located at each face of the unit cell as well as at each corner. This gives four atoms per unit cell. In the body-centered cubic unit cell, there is one atom in the center of the unit cell as well as atoms at the corners. This gives two atoms per unit.

# Solve

From Figure 12.10 we can see that the packing in the bcc unit cell is less dense (more open spaces) than in the fcc unit cell. Therefore, the fcc unit cell has greater packing efficiency.

# Think About It

The ccp and hcp structures, being closest packed, have the same packing efficiency, with 74% of the unit cell filled with atoms.

12.17. Collect and Organize

Iron can adapt either the bcc unit cell structure (at room temperature) or the fcc unit cell structure (at 1070°C). We are asked whether these two forms are allotropes.

# Analyze

Allotropes are defined as different molecular forms of an element.

# Solve

Iron is not molecular and the bcc and fcc unit cell structures describe only a difference in atom packing in the metal. Therefore, these structural forms are not allotropes.

# Think About It

Elements that do have allotropes include phosphorus, sulfur, and carbon.

12.18. Collect and Organize

We are to explain why calcium is fcc at low temperatures and bcc at higher temperatures.

# Analyze

The fcc structure is more tightly packed than the bcc structure.

# Solve

At high temperatures there is greater atomic motion than at low temperatures, so the calcium atoms might adopt the less tightly packed bcc unit cell structure at high temperatures.

# Think About It

The change in structure at the atomic level means that there are changes at the macroscopic level. For example, we might expect that a sample of calcium would expand and become less dense when heated.

12.19. Collect and Organize

Knowing that pm for the bcc structure of europium, we are to calculate the radius of one atom of europium.

# Analyze

For the bcc structure the body diagonal contains two atoms of europium, or 4r, and the body diagonal is equal to  where is the unit cell edge length, 240.6 pm.

# Solve

# Think About It

If the structure of the unit cell were simple cubic the radius of the europium atom would simply be

12.20. Collect and Organize

Using the fact that nickel crystallizes in an fcc unit cell with an edge length of 350.7 pm, we are to calculate the radius of the nickel atom.

# Analyze

In an fcc unit cell the edge length is  and the face diagonal is . The face diagonal has the atoms touching and is equal to 4r where r is the radius of the touching atoms. To determine r for nickel we can substitute  = 350.7 pm into the face diagonal relationship  = 4r.

# Solve

# Think About It

This calculated value is identical to the value of 124 pm listed in Appendix 3.

12.21. Collect and Organize

We are to calculate the edge length of the unit cell of Ba knowing that it crystallizes in a bcc unit cell and that rBa = 222 pm.

# Analyze

The body diagonal of a bcc unit cell has the relationship  An edge has the length  so all we need to do is rearrange the body diagonal expression to solve for

# Solve

# Think About It

Be careful to not assume that the edge length of every unit cell is = 2r, as in a simple cubic.

12.22. Collect and Organize

We are to calculate the edge length of the unit cell of Al knowing that it crystallizes in an fcc unit cell and 
rAl = 143 pm.

# Analyze

The face diagonal of an fcc unit cell has the relationship  = 4r. An edge has the length  so all we need to do is rearrange the face diagonal expression to solve for

# Solve

# Think About It

Be careful to not assume that the edge length of every unit cell is = 2r, as in a simple cubic.

12.23. Collect and Organize

We are to determine the type of unit cell for a form of copper using the density of the crystal (8.95 g/cm3) and the radius of the Cu atom (127.8 pm).

# Analyze

For each type of unit cell (simple cubic, body-centered cubic, and face-centered cubic), we can compare the calculated density to that of the actual density given for the crystalline form of copper. Density is mass per volume. The mass of each unit cell is the mass of the copper atoms contained in each unit cell. To find this, we first have to determine the number of atoms of Cu in each unit cell based on its structure. Then, we multiply by the mass of one atom of Cu:

The volume of each unit cell is  which is related to r in a way that depends on the type of unit cell.

# Solve

For a simple cubic unit cell where all the Cu atoms are at the corners of the cube:

Number of Cu atoms = 8   = 1 Cu atom

= 2r = 2  127.8 pm = 255.6 pm

Converting to centimeters for the calculation of density (g/cm3) gives

Volume =  = (2.556  10–8 cm)3 = 1.670  10–23 cm3

For a body-centered cubic unit cell where there is one Cu atom in the center of the unit cell and eight Cu atoms at the corners of the cube:

Number of Cu atoms = (8  ) + 1 = 2 Cu atoms

From the body diagonal 4r =  or = ,

Converting to centimeters for calculation of density (g/cm3) gives

Volume =  = (2.951  10–8 cm)3 = 2.570  10–23 cm3

For a face-centered cubic unit cell where there are eight Cu atoms at the corners of the unit cell and six on the faces:

Number of Cu atoms = (8  ) + (6  ) = 4 Cu atoms

From the face diagonal 4r =  or = ,

Converting to centimeters for calculation of density (g/cm3) gives

Volume =  = (3.615  10–8 cm)3 = 4.724  10–23 cm3

The fcc unit cell gives a density closest to the given density, so we predict that in this crystalline form of Cu the atoms pack in (c) an fcc unit cell.

# Think About It

Notice that even though the fcc unit cell has the largest edge length, the unit cell contains more atoms and so it yields the densest structure.

12.24. Collect and Organize

We are to determine the type of unit cell for a form of molybdenum using the density of the crystal (10.28 g/cm3) and the radius of the Mo atom (139 pm).

# Analyze

For each type of unit cell (simple cubic, body-centered cubic, and face-centered cubic), we can compare the calculated density to that of the actual density given for the crystalline form of molybdenum. Density is mass per volume. The mass of each unit cell is the mass of the molybdenum atoms contained in each unit cell. To find this, we first have to determine the number of atoms of Mo in each unit cell based on its structure. Then, we multiply by the mass of one atom of Mo.

The volume of each unit cell is , which is related to r in a way that depends on the type of unit cell.

# Solve

For a simple cubic unit cell where all the Mo atoms are at the corners of the cube:

Number of Mo atoms = 8   = 1 Mo atom

= 2r = 2  139 pm = 278 pm

Converting to centimeters for calculation of density (g/cm3) gives

Volume =  = (2.78  10–8 cm)3 = 2.15  10–23 cm3

For a body-centered cubic unit cell where there is one Mo atom in the center of the unit cell and eight Mo atoms at the corners of the cube:

Number of Mo atoms = (8  ) + 1 = 2 Mo atoms

From the body diagonal 4r =  or =

Converting to centimeters for calculation of density (g/cm3) gives

Volume =  = (3.21  10–8 cm)3 = 3.31  10–23 cm3

For a face-centered cubic unit cell where there are eight Mo atoms at the corners of the unit cell and six on the faces:

Number of Mo atoms = (8  ) + (6  ) = 4 Mo atoms

From the face diagonal 4r =  or = ,

Converting to centimeters for calculation of density (g/cm3) gives

Volume =  = (3.93  10–8 cm)3 = 6.07  10–23 cm3

The fcc unit cell for Mo gives a calculated density closest to the given density, so we predict that in this case Mo forms crystals packing in (c) an fcc arrangement.

# Think About It

Notice that even though the fcc unit cell has the largest edge length, the unit cell contains more atoms and so it yields the densest structure.

12.25. Collect and Organize

We may use the radius and crystal structure of sodium to determine the density of Na under high pressures.

# Analyze

Using the radius of a sodium atom, we may determine the edge length of the unit cell using the relationship

r = 0.4330 for a body centered cubic structure. We may calculate the volume by cubing the edge length, and calculate the mass of the two atoms contained in the unit cell. By dividing this mass by the calculated volume, we can determine the density of Na. Under standard conditions, the density of Na is 0.971 g/cm3. The density should be similar under high pressure.

# Solve

# Think About It

The density is near our expected value. It is important to account for both Na atoms in the bcc unit cell.

12.26. Collect and Organize

We may use the radius of calcium to calculate the density of the simple cubic phase of the metal under pressure. If we instead calculate the density of the fcc phase, then use that density for the simple cubic phase, we may calculate the radius of the calcium atoms in the simple cubic phase.

# Analyze

Using the radius of calcium from the Appendix (197 pm), we may determine the edge length of the unit cell using the relationship r = 0.5 for a simple cubic structure. We may calculate the volume by cubing the edge length, and calculate the mass of the one calcium atom contained in the unit cell. Dividing this mass by the calculated volume, we can determine the density of Ca.

We may calculate the density of the fcc phase in the same manner as in part a using the relationship 
r = 0.3536 and recognizing that the fcc unit cell contains four Ca atoms. We may determine the volume of the sc phase by dividing the volume of the sc unit cell by the density calculated for the fcc phase. The cube root of this volume is the edge length of the sc unit cell, which is related to the radius by the equation r = 0.5. The radius of calcium should be slightly smaller than 197 pm.

# Solve

(a)

(b) Calculating the density of the fcc phase

Using the density of the fcc phase, calculating the radius of the Ca atom

# Think About It

The radius calculated in (b) is roughly 89% the radius listed under standard conditions, which seems like a reasonable range. More accurate data could be obtained using X-ray crystallography.

12.27. Collect and Organize

We can use the dimensions of the hexagonal unit cell to determine the density of titanium.

# Analyze

The volume of a hexagonal unit cell may be determined using the equation

where a is the side length of the hexagon (295 pm), and h is the height of the unit cell (469 pm). Converting the cell dimensions provided in Figure P12.27 from pm to cm will yield the volume of the unit cell in cm3. The mass of Ti in the hcp unit cell may be calculated by dividing the six Ti atoms in the unit cell by Avogadro’s number and multiplying by the molar mass of titanium. The density is calculated by dividing the mass of Ti in the unit cell by the volume of the unit cell.

# Solve

# Think About It

Titanium is a relatively light and strong metal that is used for medical implants and other applications where a strong, light metal is required.

12.28. Collect and Organize

We can use the dimensions of the hexagonal unit cell to determine the density of cobalt.

# Analyze

The volume of a hexagonal unit cell may be determined using the equation

where a is the side length of the hexagon (251 pm), and h is the height of the unit cell (407 pm).

Converting the cell dimensions provided in Figure P12.27 from pm to cm will yield the volume of the unit cell in cm3. The mass of Co in the hcp unit cell may be calculated by dividing the six Co atoms in the unit cell by Avogadro’s number, and multiplying by the molar mass of cobalt. The density is calculated by dividing the mass of Co in the unit cell by the volume of the unit cell. Since the cell dimensions are smaller than those of titanium, and the molar mass of cobalt is higher than that of titanium, it is reasonable to expect that the density of Co will also be greater than Ti.

# Solve

Cobalt is nearly twice as dense as titanium.

# Think About It

Our prediction was reasonable. More mass in a smaller volume must lead to a greater density of matter.

12.29. Collect and Organize

We are asked to describe the differences between substitutional and interstitial alloys and give an example of each.

# Analyze

An alloy is a mixture of two or more metallic elements in solution with each other. The differences between substitutional and interstitial alloys involve the arrangement of atoms in the solution.

# Solve

Substitutional alloys involve replacing atoms in a lattice with atoms of another element. An example of a substitutional alloy is bronze, an alloy composed of a copper lattice containing up to 30% tin. The tin atoms may be randomly distributed throughout the bronze, occupying any lattice position normally occupied by a copper atom in pure copper metal.

Interstitial alloys contain solutes in the spaces or “holes” left when the solvent lattice formed. An example of an interstitial alloy is austenite, an alloy containing carbon atoms in the octahedral holes of the iron fcc lattice.

# Think About It

Both interstitial alloys and substitutional alloys have a range of compositions rather than fixed ratios of components.

12.30. Collect and Organize

We can use the definitions of intermetallic compounds and homogeneous alloys to describe the similarities and differences between these terms.

# Analyze

An alloy is a mixture of two or more metallic elements in solution with each other. An intermetallic compound is an alloy with a reproducible stoichiometry.

# Solve

Both are homogeneous mixtures of solids. There is a subtle difference, however. An alloy is a mixture of two or more metallic elements, and an intermetallic compound is an alloy with a defined composition.

# Think About It

All alloys are solid solutions, but not all solid solutions are alloys.

12.31. Collect and Organize

We are asked what effect the substitution of one Ni atom at the center of the bcc Ti unit cell would have on the edge length of the crystal.

# Analyze

From the appendix, we find that Ni has a radius of 124 pm and Ti has a radius of 147 pm. In a bcc unit cell, atoms touch along the body diagonal, but not directly along an edge.

# Solve

Ni is smaller than Ti. By substituting a nickel atom for a titanium atom, the body diagonal will be shorter, and thus, the unit cell will be smaller than that for pure titanium. The edge length for NiTi will be smaller than for Ti alone.

# Think About It

Using the same logic, we could also predict that the unit cell for NiTi will be larger than that for pure Ni.

12.32. Collect and Organize

Given that white gold is an alloy of Au and Ni, we are asked whether it is more malleable than pure Au.

# Analyze

When other metals are alloyed into a pure metal, the atomic structure of the metal is changed so that the atoms are not in as regular an arrangement as in the pure metal.

# Solve

The disruption of the gold lattice by the smaller Ni atoms in white gold restricts the gold atoms from slipping past each other as easily as in pure gold. Therefore, pure gold is more malleable.

# Think About It

Pure gold is too soft to be used for jewelry, so it is alloyed with other metals such as nickel to make it more durable.

12.33. Collect and Organize

We are asked to decide if including hafnium atoms in place of magnesium atoms will generate an alloy with a greater or lesser density than pure magnesium.

# Analyze

The size of the hafnium and magnesium atoms are nearly identical, so we can assume that there are no distortions to the unit cell when this substitution occurs. The atomic mass of magnesium is 24.3050 amu, and the atomic mass of hafnium is 178.49 amu.

# Solve

The significant increase in mass when hafnium is substituted for magnesium will result in an alloy of greater density than that of pure magnesium.

# Think About It

The density of the resulting alloy will be less than that of pure hafnium.

12.34. Collect and Organize

We consider here why alloys of transition metals with the second-row nonmetals B, N, and C are interstitial rather than substitutional alloys.

# Analyze

Substitutional alloys generally have atomic radii of the alloying elements within 15% of each other. The sizes of the transition metals are in the range of 124–180 pm (Appendix 3) and the radii of B, C, and N are in the range of 75–88 pm (Appendix 3).

# Solve

The radius ratio of these alloys fall in the range

These ratios are significantly smaller than the 0.85 or higher ratio for substitutional alloys. Therefore, the large difference in atomic sizes accounts for the alloying elements occupying interstitial rather than substitutional lattice sites.

# Think About It

According to the ratio range calculated above for these alloys, we predict that B, N, and C occupy octahedral holes in the closest-packed lattices of transition metals.

12.35. Collect and Organize

We are to compare the two unit cells in Figure P12.35 and decide if both are accurate depictions of NiTi.

# Analyze

For a bcc unit cell, 1/8 of an atom is located in the cell at each corner, and an entire atom is located in the center. For the diagram to be accurate, the unit cells much each produce a 1:1 ratio of Ni:Ti.

# Solve

For 8 X atoms at the corners and 1 Y atoms in the center of the unit cell:

Both unit cells produce the same ratio of Ni to Ti, so both are valid.

# Think About It

This alloy structure is similar to the bcc unit cell of CsCl.

12.36. Collect and Organize

We are to compare the two unit cells in Figure P12.36 and decide if both are possible depictions of the same substitutional alloy.

# Analyze

For an fcc unit cell, 1/8 of an atom is located in the cell at each corner, and 1/2 an atom is located on each face. If the ratio of atoms in the left and right diagrams are the same, the depictions are equivalent. We can assume the yellow spheres represent Au atoms and the bronze spheres represent Cu atoms.

# Solve

The ratio of atoms does not match, so the two diagrams are not equivalent.

# Think About It

The diagram on the left represents the rose gold substitutional alloy, with 25% copper content.

12.37. Collect and Organize

By substituting the radius of hydrogen into the radius ratio for the tetrahedral holes of an fcc unit cell, we may determine the range of metal hosts that could form an interstitial alloy with hydrogen. We are asked to determine if the interstitial alloy formed as a result of hydrogen present in the form of a hydride ion would more likely occupy octahedral or tetrahedral holes in the host metal.

# Analyze

For the fcc unit cell, the acceptable range of host and nonhost radii is

rnonhost/rhost = 0.22 – 0.41

The radius of the hydrogen atom (the nonhost) is 37 pm. The ratio of 0.41 represents the smallest difference between hydrogen and the metal. This gives the minimum radius the metal could have for hydrogen to fit into tetrahedral holes of the fcc lattice.

# Solve

(a) The smallest metal host radius that would form such an alloy is

(b) The radius of the hydride ion (146 pm) is closer to that of most metals. The hydride ion is more likely to form a substitutional alloy.

# Think About It

Even if the hydride ion were to occupy the octahedral holes of a metal, the metal would have to have a radius of  >200 pm!

12.38. Collect and Organize

We are to determine the minimum radius of an atom that can accommodate boron (88 pm) in octahedral holes. To answer this we can use the highest value of the ratio range for octahedral holes (Table 12.4). We are also asked to determine the molecular formula given an average occupancy of one boron atom per unit cell.

# Analyze

To fit in an octahedral hole the radius of boron divided by the atom’s radius must be between 0.41 and 0.73. The ratio of 0.41 represents the largest difference between boron and the atom. The ratio of 0.73 represents the smallest difference between boron and the atom. This gives the minimum radius the atom could have for boron to fit into octahedral holes of the closest-packed atoms. The fcc unit cell contains four octahedral holes, and four metal atoms per unit cell.

# Solve

(a)

(b) If one octahedral hole is occupied per unit cell, the ratio of metal to boron will be M4B1, or MB0.25.

# Think About It

The maximum radius that would hold boron in an octahedral hole would use 0.41 in the calculation. Using that value, the radius of the atom would be 215 pm.

12.39. Collect and Organize

By calculating the radius ratio of Sn to Ag, we can determine whether dental alloys of Sn and Ag are substitutional or interstitial alloys.

# Analyze

It would be possible for an alloy to be both interstitial and substitutional as long as the voids within the lattice are about the same size as the metal atom. In particular, if the host metal has a simple cubic structure, the alloying metal may fit in a cubic void (radius ratio > 0.73) as well as substitute for the host metal in the lattice structure.

# Solve

Because these radii are within 15% of each other, an alloy of silver and tin is a substitutional alloy.

# Think About It

Remember that it is also important for the metals in substitutional alloys to crystallize in the same closest-packed (hcp, ccp, simple cubic, bcc) structures.

12.40. Collect and Organize

We can compare the difference in atomic size for Sn3Hg and for bronze made of Cu and Sn to determine which alloy has a smaller mismatch.

# Analyze

We can use the ratios of the atomic radii to answer this question. We are given the radii for tin (140 pm) and mercury (151 pm). The radius of the copper atom is listed in Appendix 3 as 128 pm.

# Solve

For Sn3Hg

For bronze

Sn3Hg has a smaller mismatch in atomic size.

# Think About It

Both alloys are substitutional because the elements’ radii are within 15% of each other.

12.41. Collect and Organize

We are to predict the formula of vanadium carbide if the vanadium lattice is ccp (fcc), and two octahedral holes are occupied by carbon atoms.

# Analyze

The fcc arrangement of V atoms has four atoms of V in the unit cell. This fcc unit cell also contains four octahedral holes and eight tetrahedral holes.

# Solve

If only two of the four octahedral holes are occupied, the ratio of atoms in this lattice is V4C2, or V2C.

# Think About It

If all of the octahedral holes were filled, the formula of the alloy would be VC.

12.42. Collect and Organize

We are to predict the formula of manganese nitride if the manganese lattice is ccp (fcc), and one tetrahedral hole is occupied by a nitrogen atom.

# Analyze

The fcc arrangement of Mn atoms has 4 atoms of Mn in the unit cell. This fcc unit cell also contains four octahedral holes and eight tetrahedral holes.

# Solve

If only one of the eight tetrahedral holes are occupied, the ratio of atoms in this lattice is Mn4N.

# Think About It

If all of the tetrahedral holes were filled, the formula of the alloy would be MnN2.

12.43. Collect and Organize

We can use the radii of Ni and Ti to calculate the density of the nitinol alloy.

# Analyze

Nitinol is an alloy composed of one Ni atom and one Ti atom per bcc unit cell. The radii of Ni (124 pm) and Ti (147 pm) may be used to calculate the body diagonal for the bcc unit cell:

We may then use the relationship below to determine the edge length of the unit cell:

Cubing the edge length yields the volume of the unit cell. We may determine the mass of the unit cell by multiplying the number of each atom by its molar mass and dividing by Avogadro’s number. The density is obtained by dividing this mass by the volume of the unit cell determined above.

# Solve

Calculating the volume of the unit cell:

The mass of the unit cell is

The density of nitinol is

# Think About It

The calculated density for nitinol is reasonable for this alloy of two first row transition metals.

12.44. Collect and Organize

We can use the radii of Cu and Au to calculate the density of the rose gold alloy.

# Analyze

We can use a weighted average of the radii for Au (144 pm, 75%) and Cu (128 pm, 25%) to calculate the edge length of the fcc unit cell using the relationship r = 0.3536. The fcc unit cell contains four atoms, which equates to three Au atoms for every one Cu atom. By adding the masses of these atoms, we may determine the mass of the unit cell. The density of rose gold is obtained by dividing the mass of the unit cell by the volume calculated.

# Solve

Calculating the volume of the unit cell

The mass of the unit cell is

The density of nitinol is

# Think About It

The density of rose gold is much higher than that calculated for nitinol in Problem 12.43. This makes sense because gold is much heavier than the first row elements Ni and Ti.

12.45. Collect and Organize

We are asked to determine the type of structure depicted in Figure P12.45 and the relative proportions of each element present in the unit cell.

# Analyze

Figure P12.45 depicts a body-centered cubic unit cell with opposite corners occupied by Cu atoms, and the remainder of the lattice positions occupied by Zn atoms. For a bcc unit cell, at each corner 1/8 of an atom is located in the cell, and an entire atom is located in the center.

# Solve

(a) The unit cell depicted in Figure P12.45 is a bcc unit cell. The alloy is a substitutional alloy, in which some of the lattice positions of the Zn unit cell are occupied by Cu atoms.

(b) The proportions of Cu and Zn in this lattice are

The ratio of atoms is Cu0.5Zn1.5, or CuZn3.

# Think About It

Though rose gold (see Problem 12.44) and the CuZn alloy described in this problem have the same ratio of component elements, they adopt different unit cells.

12.46. Collect and Organize

We are asked to determine if the alloy depicted in Figure P12.46 is a substitutional or an interstitial alloy. We can determine the composition of the alloy by analyzing the ratio of atoms in this lattice.

# Analyze

Figure P12.46 depicts a repeating bcc lattice of grey atoms, with four green atoms substituted for the central grey atoms. From Figure 12.7, we see that Al adopts an fcc lattice, and Fe adopts a bcc lattice. For a bcc unit cell, 1/8 of an atom is located at each corner in the cell, and an entire atom is located in the center.

# Solve

(a) The alloy depicted in Figure P12.46 is a substitutional alloy, in which the half of the central grey atoms have been replaced by green atoms.

(b) By matching the unit cell to that predicted for the pure elements, we may assume that the grey atoms are Fe, and the green atoms are Al. Over the eight adjoining unit cells, the occupancy is

The ratio of atoms is 4(1.5 Fe atoms) + 4 (1.5 Fe atoms + 1 Al atom) = Fe12Al4, or Fe3Al.

# Think About It

The repeating unit of this alloy is a group of eight adjacent bcc unit cells.

12.47. Collect and Organize

We are to explain how the sea-of-electrons model accounts for the electrical conductivity of gold.

# Analyze

In the sea-of-electrons model the metal atoms exist in the structure as cations with their ionized electrons not associated with particular metal ions.

# Solve

Because the electrons are free to distribute themselves throughout the metal, the application of an electrical potential across the metal causes the electrons to travel freely toward the positive terminal. This movement of electrons in the structure is electrical conductivity.

# Think About It

Metals have low ionization energies. This makes the electron sea somewhat easy to achieve in the lattice of metals.

12.48. Collect and Organize

We are to explain how the high electrical conductivity of mercury is explained using band theory.

# Analyze

Band theory describes the banding in solids using valence bands and conduction bands.

# Solve

In metals, the valence band overlaps with the conduction band, which allows electrons to freely migrate to and become mobile in the conduction band.

# Think About It

Semimetals have a small band gap between the valence band and the conduction band, so only some of the electrons in the valence band have sufficient energy to move up to the conduction band.

12.49. Collect and Organize

Given that the melting and boiling points of Na are lower than those of NaCl, we are to predict the relative strengths of metallic and ionic bonds.

# Analyze

Solid sodium is held together by metallic bonds, whereas sodium chloride is held together by ionic bonds. The higher the melting point or boiling point of a substance, the stronger the forces between particles of that substance.

# Solve

Because the melting point and boiling point of NaCl are higher than those of Na, ionic bonds must be stronger than metallic bonds.

# Think About It

Some metallic bonds are quite strong, as evidenced by the melting points of some metals. Sodium has a melting point of 97.72°C, whereas tungsten melts at 3422°C.

12.50. Collect and Organize

We are asked whether Al or Na will have the higher melting point.

# Analyze

The more valence electrons a metal can share, the greater the metallic bonding, and the higher the expected melting point.

# Solve

Aluminum should have the higher melting point because it has three valence electrons to share with its neighbors in the metallic structure, giving it stronger metallic bonding capability than Na, which has only one valence electron. The stronger the metallic bond, the higher the melting point.

# Think About It

Our prediction is correct. The melting point of aluminum (660.32°C) is greater than that of sodium (97.72°C).

12.51. Collect and Organize

We are to consider whether band theory can explain why hydrogen at very low temperatures and high pressures might act like a metal and conduct electricity.

# Analyze

Band theory is a model of bonding in which orbitals on many atoms are combined, as in molecular orbital theory, to form a fully or partially filled valence band and an empty conduction band.

# Solve

Yes, by combining the 1s orbitals on many hydrogen atoms at very low temperatures and at high pressures, we could construct a molecular orbital diagram that would show a partially filled valence band (as for copper in Figure 12.20) in which the electrons can move into the unfilled portion of the band where they can migrate freely.

# Think About It

Metallic liquid hydrogen was discovered with hydrogen at very low temperatures and very high pressures in 1996 at the Lawrence Livermore National Laboratory quite by accident.

12.52. Collect and Organize

Using band theory we can consider whether to expect solid helium to conduct electricity.

# Analyze

Band theory is a model of bonding in which orbitals on many atoms are combined, as in molecular orbital theory, to form a fully or partially filled valence band and an empty conduction band.

# Solve

Under high pressure and low temperature, the filled 1s orbitals on many He atoms would form a filled valence band. The next orbitals in energy, the 2s orbitals, could form the conduction band. If the conditions are such that the valence band and the conduction band overlap (as shown in Figure 12.21 for zinc), then solid helium could conduct electricity.

# Think About It

Like metallic hydrogen, we might expect metallic helium to form under very high pressures.

12.53. Collect and Organize

We are asked to identify which groups in the periodic table contain metals with filled valence bands.

# Analyze

The metals in the periodic table are in groups 1–12, with some in group 13 (Al, Ga, In, TI), group 14 (Si, Ge, Sn, Pb), group 15 (As, Sb, Bi), group 16 (Te, Po), and group 17 (At). Filled valence bands for metals occur for electron configurations of ns2 and nd10.

# Solve

Metals of groups 2 and 12 have filled valence bands.

# Think About It

The orbital energy diagram for these metals will be similar to that of zinc in Figure 12.21.

12.54. Collect and Organize

We are asked to rank semiconductors, insulators, and conductors in order of increasing band gap.

# Analyze

The band gap is the energy difference between the occupied valence band and the empty conduction band. Conductors have overlapping bands, semiconductors have a relatively small band gap through which some electrons can be promoted from the valence band to the conduction band, and insulators have large band gaps, which prohibit valence band electrons from moving into the conduction band.

# Solve

In order of increasing band gap: conductor < semiconductor < insulator.

# Think About It

Because of their overlapping valence and conduction bands, metals very easily conduct both heat and electricity.

12.55. Collect and Organize / Analyze

We are asked to describe the differences between n-type and p-type semiconductors. n-Type semiconductors have a small quantity of dopant with more valence electrons than the metalloid, whereas p-type semiconductors have a small quantity of dopant with fewer valence electrons than the metalloid.

# Solve

Doping a metalloid generates a semiconductor with a smaller band gap than the starting material. n-Type semiconductors have “extra” electrons that are higher in energy than the valence band for the undoped material. p-Type semiconductors have “extra” holes that are lower in energy than the conduction band for the undoped material. In both types of doped semiconductor the effect is similar—the band gap is lowered, and electrons may flow through the material with greater ease than in the undoped metalloid.

# Think About It

Phosphorus, with one more electron than silicon, would form an n-type semiconductor if it were present as a dopant in silicon. Aluminum, with one fewer electron than silicon, would form a p-type semiconductor if it were present as a dopant in silicon.

12.56. Collect and Organize

We are asked how the presence of germanium in silicon might change the conductivity of the silicon.

# Analyze

Germanium and silicon have the same number of valence electrons because they are in the same group in the periodic table. Germanium and silicon do have different ionization energies (germanium’s first ionization energy is 762.2 kJ/mol and silicon’s is 786.5 kJ/mol).

# Solve

Because germanium holds its electrons less tightly, as indicated by its lower ionization energy, its presence in silicon might enhance the electrical conductivity of silicon.

# Think About It

Because Ge has the same number of valence electrons as Si, it is neither a p- nor an n-type dopant for silicon.

12.57. Collect and Organize

We are asked to identify in which group of the periodic table we might find elements that would be useful to form a p-type semiconductor with Sb2S3.

# Analyze

Antimony has five valence electrons, and sulfur has six valence electrons. To form a p-doped semiconductor, we would choose elements with fewer than five valence electrons.

# Solve

Group 14 elements with four valence electrons would form p-type semiconductors when doped into Sb2S3.

# Think About It

Similarly, group 13 elements, with three valence electrons, might also be used to form p-doped Sb2S3 semiconductors.

12.58. Collect and Organize

We are to determine which group of elements would be the best for doping Sb2S3 to form an n-type semiconducting material.

# Analyze

Doping with elements that contribute an extra electron to the structure gives an n-type semiconductor. Sb2S3 is composed of a group 15 and a group 16 element. Antimony has five valence electrons, and sulfur has six valence electrons.

# Solve

Extra electrons would be brought to the structure by doping in a halogen (group 17), which would bring seven valence electrons to the structure of the semiconductor.

# Think About It

A p-type semiconductor of Sb2S3 would be possible by doping in elements of group 14 (Si, Ge, Sn, Pb).

12.59. Collect and Organize

We consider the properties of nitrogen-doped diamond.

# Analyze

(a) Nitrogen, with five valence electrons, has one more electron than carbon, with four valence electrons.

(b) In diamond, the valence band and the conduction band are separated by a large band gap, making diamond an insulator. Adding nitrogen to the diamond structure adds a partially filled band above diamond’s valence band and below its conduction band.

(c) Because E = hc/, we can calculate the energy of the band gap when  = 4.25  10–7 m.

# Solve

(a) Because nitrogen has one more valence electron than carbon, nitrogen serves as an n-type dopant in diamond.

(b)

(c)

# Think About It

Because nitrogen-doped diamonds absorb violet light, we observe a yellow color (the complement of violet) in the diamond.

12.60. Collect and Organize

Boron in diamond gives it a blue color. We are to determine whether diamond with boron impurities is n-type or p-type, then draw a scheme showing the band structure for doped and undoped diamond, and compute the band gap energy given the wavelength of light absorbed by the boron-doped blue diamond.

# Analyze

(a) Diamonds are composed of carbon, which has four valence electrons. Boron has three valence electrons.

(b) Diamond is an insulator so its band gap is large. Doping the diamond places an energy level (either filled for n-type or unfilled for p-type) in the band gap of the diamond.

(c) The band gap energy is directly related to the wavelength absorbed. To calculate Eg, we need to use the equation relating energy to wavelength:

# Solve

(a) Because boron has one fewer valence electron than carbon, the B-doped diamond is an example of a p-type semiconductor.

(b)

(c)

# Think About It

Diamond semiconductors doped with boron have indeed been made. The advantage of using diamond as a semiconducting material is that it would be able to very efficiently dissipate the heat generated in a transistor.

12.61. Collect and Organize

We are asked to determine the effect of increased pressure on the wavelength of light emitted by ZnS. For this material, the band gap increases with increasing pressure.

# Analyze

The wavelength of light absorbed or emitted by a semiconductor is inversely related to the band gap energy:

To calculate the wavelength we can rearrange this equation to

# Solve

As the band gap increases with increasing pressure, the wavelength of light emitted will decrease.

# Think About It

Wavelength is inversely proportional to energy. A smaller wavelength corresponds to more energetic (blue-shifted) light.

12.62. Collect and Organize

Given the band gap energies of AlP, GaP, and InP, we are to calculate the wavelengths of light emitted by these semiconductors.

# Analyze

The wavelength of light emitted by a semiconductor is directly related to the band gap energy:

To calculate the wavelength we can rearrange this equation to

The wavelength is expressed in terms of a single photon, so we have to convert the energy units (from kJ/mol to J/photon).

# Solve

# Think About It

These wavelengths correspond to the visible colors blue-green (AlP) and yellow-green (GaP) and to the infrared portion (InP) of the electromagnetic spectrum.

12.63. Collect and Organize

We are to explain why the Cl– ions in the rock salt structure of LiCl touch in the unit cell, but those in KCl do not.

# Analyze

In the fcc rock salt lattice, the alkali metal, Li+ or K+, is placed into the octahedral holes of the unit cell. From the radius ratio rule applied to LiCl and KCl (ionic radii are given in Figure 10.2),

# Solve

The radius ratios show that K+ is large and so does not fit well into the octahedral holes (radius ratio between 0.41 and 0.73). Therefore, the rock salt structure for KCl has Cl– ions that may not touch in order to accommodate the large K+ ions in the fcc lattice.

# Think About It

The radius ratio rule is simply a guide to predicting in which type of hole cations will fit within the anion lattice. You will find that sometimes we would predict an octahedral hole for a cation when the actual crystal places the cation into a cubic hole, for example.

12.64. Collect and Organize

We are asked if the size of the octahedral holes changes as we consider the lattices of the halogens from fluorine to iodide (i.e., down the group).

# Analyze

As we descend the halogens, the principal quantum number increases, leading to an increase in atomic radius. To help envision the alterations to the structure that occur when we increase the atomic radius, imagine an fcc lattice comprised of baseballs, compared to the same lattice comprised of basketballs.

# Solve

While the ratio of volume occupied by atoms and holes is unaltered, the absolute size of the holes increases with increasing radius. The iodide lattice will contain larger holes.

# Think About It

We also see this trend when considering the ratio of host and nonhost radii in Table 12.4. Though the radius ratio will remain the same for a given lattice, the size of the guest may increase with increasing host atom radius.

12.65. Collect and Organize

We are to describe how CsCl could be viewed as both a simple cubic and a body-centered cubic structure.

# Analyze

A simple cubic structure consists of atoms located only at the corners of a cube. A body-centered cubic structure consists of an atom inside a cube of atoms.

# Solve

The radius of Cl– is 181 pm and the radius of Cs+ is 170 pm and so their radii are very similar. The Cs+ ion at the center of Figure P12.65 occupies the center of the cubic cell, so CsCl could be viewed as a body-centered cubic structure when taking into account the ions’ slight difference in size. However, if we look at the ions as roughly equal in size, the unit cell becomes two interpenetrating simple cubic unit cells.

# Think About It

In the body-centered cubic unit cell, the cubic hole in the simple cubic unit cell is filled.

12.66. Collect and Organize

We are asked to consider what changes to the lattice of ZnS would occur if some of the S2– ions were replaced with Se2– ions.

# Analyze

The radii of S2– and Se2– are 184 pm and 198 pm, respectively, and the radius of Zn2+ is 74 pm. The structure of ZnS is an fcc lattice of S2– ions with Zn2+ ions in four of the eight tetrahedral holes. The acceptable ratio of radii for an ion occupying a tetrahedral hole in an fcc unit cell is

Comparing the radius ratio for the extreme cases (ZnS and ZnSe) will reveal whether the structure must change to accommodate the change in ion size.

# Solve

For ZnS, the radius ratio is

For ZnSe, the radius ratio is

Both of these lie within the acceptable range for Zn2+ occupying the tetrahedral holes of an fcc host lattice. Yes, the Se2– ions should occupy the same sites at the S2– ions.

# Think About It

The difference in the ratio of S and Se is approximately 8%, which is within the acceptable tolerance of 15%.

12.67. Collect and Organize

We can use the radius ratio rule and the formula for the salt to determine whether CaCl2 could have a rock salt structure.

# Analyze

From Figure 10.2, the radius of Cl– is 181 pm and the radius of Ca2+ is 100 pm. The radius ratio is therefore

# Solve

The radius ratio of Ca2+ and Cl– shows that the Ca2+ ions would fit into the octahedral holes of an fcc lattice of Cl– anions. However, this structure would not be like NaCl, where all the octahedral holes are filled in the fcc lattice. To balance charge, only half of the octahedral holes are filled in CaCl2.

# Think About It

CaCl2 does not have a structure like CaF2, in which the Ca2+ ions form an fcc array into which the F– ions fill all the octahedral holes. Instead it adopts a rutile, TiO2, structure.

12.68. Collect and Organize / Analyze

We are asked to account for the different structures of NaF and CaF2.

# Solve

NaF has a 1:1 ratio of ions, and CaF2 has a 1:2 ratio of ions. The same unit cell cannot accommodate both of these ion ratios.

# Think About It

The ratio of atoms or ions in the unit cell must match the ratio of atoms or ions in the bulk compound.

12.69. Collect and Organize

Given that the unit cell edge length for an alloy of Cu and Sn is the same as that for pure Cu, we are to determine whether the alloy would be more dense than pure Cu.

# Analyze

Density is mass per volume. If the unit cell edge length is the same for both the alloy and pure copper, then the volumes of the unit cells of both substances are the same. The density would be greater only if the mass of the unit cell alloy is greater than for the pure copper.

# Solve

Because tin has a greater molar mass than copper, the mass of the unit cell in the alloy would be greater and therefore, yes, the density of the alloy would be greater than the density of pure copper.

# Think About It

The unit cell volume does not change much for substitutional alloys because the alloying atoms are close in size (within 15%) to the atoms being replaced.

12.70. Collect and Organize

Assuming the unit cell edge length does not change, we are to predict whether the alloy has a greater density if carbon is placed into the interstices of the vanadium lattice.

# Analyze

Density is mass per volume. If the unit cell edge length is the same for both the alloy and pure vanadium, then the volumes of the unit cells of both substances are the same. The density would be greater only if the mass of the unit cell alloy is greater than for the pure vanadium.

# Solve

Because carbon is being added to the interstices in the closest-packed vanadium structure, the mass of the unit cell increases. Therefore, yes, the density of the alloy is greater than that of pure vanadium.

# Think About It

Interstitial alloys have small atoms as alloying elements so as to fit into the octahedral or tetrahedral holes of the closest-packed layer of larger metal atoms.

12.71. Collect and Organize

We are to predict the effect on density of an ionic compound of rock salt structure as the cation–anion radius ratio increases.

# Analyze

When the cation–anion ratio increases, the cation is increasing, relatively, in size. If the anions remain in the rock salt structure, they might have to expand the fcc structure to accommodate larger cations.

# Solve

As the cation–anion radius ratio increases, the closest-packed anions would expand so as to maintain the cations in the octahedral holes of the fcc lattice. The cell volume, therefore, increases and the calculated density would be less than the measured density.

# Think About It

Another factor in density is the molar mass of the ions of the structure.

12.72. Collect and Organize

We are to predict the effect on the unit cell edge length for an ionic compound with the rock salt structure as the cation–anion radius ratio increases.

# Analyze

As the cation–anion radius ratio increases, the closest-packed anions may have to expand to accommodate the larger cations in the octahedral holes of the fcc structure.

# Solve

As the cation–anion radius ratio increases, the expansion of the unit cell to accommodate the larger cations means that the calculated edge length  from the fcc unit cell along the body diagonal) will be less than the observed edge length because larger cations in the octahedral holes cause the anions along the face diagonal to no longer touch.

# Think About It

In more advanced texts, several radii are provided in tables for cation size. Often radii are listed for the cation in tetrahedral, octahedral, and cubic holes. Sometimes the size differences between the same ions, but different holes, are substantial.

12.73. Collect and Organize

For a ccp array of O2– ions with  of the octahedral holes containing Fe3+,  of the tetrahedral holes containing Fe3+, and  of the octahedral holes containing Mg2+, we are asked to write the formula of the ionic compound.

# Analyze

In a ccp array of ions, there are four octahedral holes and eight tetrahedral holes. The ccp array has an fcc unit cell which has four closest-packed anions.

# Solve

The unit cell will have the following:

4 O2– anions in the fcc unit cell

1 Fe3+ in octahedral holes

1 Fe3+ in tetrahedral holes

1 Mg2+ in octahedral holes

The formula is MgFe2O4.

# Think About It

The salt has charge balance as well: 4 O2– gives a charge of 8–, which is balanced by 2 Fe3+ plus 1 Mg2+ or a charge of 8+.

12.74. Collect and Organize

We are to deduce the formula of the compound in which Ba2+ occupies half of the cubic holes in a simple cubic arrangement of F– anions.

# Analyze

The number of cubic holes in the simple cubic unit cell is one. The number of F– anions in the unit cell is also one.

# Solve

Because the Ba2+ occupies half of the cubic holes in the structure, it is helpful to consider two unit cells. Two unit cells have 2 F– anions and two cubic holes, one of which is occupied by the Ba2+ cation. Therefore, the formula of the compound is BaF2.

# Think About It

Ba2+ occupies only half of the cubic holes in the structure of this compound in order to maintain charge balance.

12.75. Collect and Organize

We consider the structure of anatase, a form of TiO2, found on a map of Vinland believed to date from the 1400s.

# Analyze

We can predict the type of hole Ti4+ is likely to occupy by calculating the radius ratio  The radius ratios for tetrahedral, octahedral, and cubic holes are 0.22–0.41, 0.41–0.73, and 0.73–1.00, respectively (Table 12.4). In the ccp structure the unit cell is fcc. This unit cell contains four octahedral and eight tetrahedral holes.

# Solve

(a) From the radius ratio,

Ti4+ is expected to occupy octahedral holes.

(b) To give charge balance there is one Ti4+ ion for every two O2– ions in the lattice. Because the unit cell contains 4 O2– ions, there must be 2 Ti4+ ions in the unit cell. Since there are four octahedral holes in the unit cell, this must mean that half of the octahedral holes in the unit cell are occupied.

# Think About It

If the Ti4+ were small enough to fit into the tetrahedral holes, then one-fourth of the tetrahedral holes would be occupied.

12.76. Collect and Organize

Given the ccp structure of the O2– anions in olivine (M2SiO4) and the fact that Si4+ cations occupy the tetrahedral holes and M2+ cations occupy the octahedral holes in the structure, we are to calculate the fraction of tetrahedral and octahedral holes that are occupied and consider why the unit cell volumes differ between Mg2SiO4 and Fe2SiO4.

# Analyze

The ccp structure has an fcc unit cell. This cell contains four O2– ions with four octahedral holes and eight tetrahedral holes. Because the unit cell contains four O2– ions, the same as the formula for olivine, we need only look at one unit cell.

# Solve

(a) Because there is one Si4+ ion in the formula there is one of these ions in one of the tetrahedral holes in the unit cell. The fraction of tetrahedral holes occupied, therefore, is one-eighth. There are two M2+ ions in the unit cell distributed among four octahedral holes. The fraction of octahedral holes that are occupied, therefore, is 2/4, or one-half.

(b) The Fe2+ cation is larger than Mg2+. Even though they both fit in octahedral holes in the structure, the larger Fe+2 ions expand the lattice of O2– ions slightly, giving Fe2SiO4 a larger unit cell volume.

# Think About It

If the Si4+ ions were located in the octahedral holes, then one-fourth of the octahedral holes would be occupied. The M2+ ions would then occupy one-fourth of the tetrahedral holes.

12.77. Collect and Organize

We are asked to identify the differences between the rock salt and cesium chloride structures and explain how both structures are a suitable match for MgSe.

# Analyze

In the rock salt structure, the Se2– ions would be in an fcc array, with Mg2+ occupying all of the octahedral holes. In the cesium chloride structure the Se2– ions are in a simple cubic array, with Mg2+ ions occupying the cubic holes.

# Solve

(a) The rock salt and cesium chloride lattices have the same ratio of ions, but the relative arrangements differ. In the rock salt structure, the Se2– ions would be in an fcc array, with Mg2+ occupying all of the octahedral holes. In the cesium chloride structure the Se2– ions are in a simple cubic array, with Mg2+ ions occupying the cubic holes.

(b) Both structures have the same ratio of Mg to Se.

For the rock salt structure, the ratio is Mg4Se4, or MgSe:

For the cesium chloride structure, the ratio is MgSe:

# Think About It

We can also imagine the rock salt structure like two interpenetrating fcc lattices, and the cesium chloride structure like two interpenetrating simple cubic lattices.

12.78. Collect and Organize

We are asked to identify the differences between the rock salt form of ZnS and the sphalerite form and explain how both structures are consistent with the stoichiometry of ZnS.

# Analyze

Both the rock salt and sphalerite forms of ZnS have an fcc unit cell of S2– ions. They differ only in which holes are occupied in the unit cell, namely, octahedral or tetrahedral, respectively. We can compare the ratio of ions in each structure.

# Solve

(a) The rock salt  form of ZnS has an fcc arrangement of S2– ions with all of the four octahedral holes in the unit cell occupied by Zn2+. The sphalerite  form of ZnS also has an fcc arrangement of S2– ions, but with half of the eight tetrahedral holes in the unit cell occupied by Zn2+.

(b) Both structures support the same ratio of Zn to S.

For the rock salt structure, the ratio is Zn4S4, or ZnS:

For the sphalerite structure, the ratio is Zn4S4, or ZnS:

# Think About It

The Zn2+ ions move from the tetrahedral holes to the larger octahedral holes under high pressure.

12.79. Collect and Organize

Knowing the structure of the unit cell of ReO3 and the radii of Re and O atoms (given as 137 pm and 73 pm, respectively), we are asked to calculate the density of ReO3.

# Analyze

Given that there are Re atoms at each corner of the cubic unit cell, there is , or 1 Re atom, in the unit cell. Likewise, given that there are 12 edge O atoms, there are  O atoms in the unit cell. We are told that the atoms touch (Re–O–Re) along an edge of the unit cell, therefore the cell edge length is

137 + 73 + 73 + 137 = 420 pm

To calculate the density of ReO3 we use

# Solve

The mass, m, of atoms in a unit cell of ReO3 is

The volume, V, of the unit cell (in cm3) is

The density, d, of the solid is then

# Think About It

Remember that this is a calculated, or theoretical, density. The actual density, even if the structure is correctly described, may differ slightly from the theoretical value.

12.80. Collect and Organize

CsCl crystallizes in a bcc unit cell with an edge length of 412 pm (Figure P12.65). Knowing this along with the molar mass of CsCl, we can calculate the density of the CsCl crystal.

# Analyze

Density is mass per volume. The volume of the unit cell is the cube of the edge length . This we should express in units of cubic centimeters for writing the density (in g/cm3). The mass of the atoms in the unit cell is the mass of one Cs+ ion and one Cl– ion. We have to express mass in terms of grams per atom, converting from grams per mole.

# Solve

# Think About It

Remember that a body-centered cubic structure contains a total of two atoms. For CsCl, the unit cell contains just one Cl– and one Cs+.

12.81. Collect and Organize

Given the structure (rock salt) and density (3.60 g/cm3) of MgO, we are asked to calculate the length of the edge of the unit cell .

# Analyze

The volume of the unit cell is simply. From the density we can calculate the volume, V, as

From the volume of the cubic unit cell, where the lengths of all the edges are equal, we can calculate the edge length

In the fcc unit cell there are four Mg atoms and four O atoms to give a mass, m, of

# Solve

# Think About It

This value seems reasonable. The radius of an oxygen atom is 73 pm and that of a manganese atom is 127 pm (Appendix 3). Assuming that the O–Mn–O atoms touch along the fcc unit edge length (a good first approximation), the edge length would be

73 + 127 + 127 + 73 = 400 pm

12.82. Collect and Organize

Given the crystalline structure of KBr (rock salt, which is fcc in Cl– with Na+ in all of the octahedral holes) and its density (2.75 g/cm3), we can calculate the length of an edge of the unit cell.

# Analyze

The rock salt structure for KBr means that there are four Br– ions and four K+ ions in the unit cell. From the density and the mass of the atoms in the unit cell we can calculate the volume of the unit cell:

From the volume of the cubic unit cell, where the lengths of all the edges are equal, we can calculate the edge length

The edge length should be expressed in picometers.

# Solve

# Think About It

We can calculate the Br– radius from this now. For an fcc crystal 4r = = 660 pm = 933 pm. The radius of Br– in this crystal is then 933 pm/4 = 233 pm.

12.83. Collect and Organize

To answer why black phosphorus has puckered rings when graphite has planar rings, we need to consider the hybridization of the phosphorus and carbon atoms that make up these two substances.

# Analyze

In both substances, the atoms are each bound to two other atoms. The phosphorus atom brings five valence electrons to its structure, but carbon brings only four to its structure.

# Solve

- The hybridization of the phosphorus atom in black phosphorus is sp3 with bond angles of 102° to give a puckered ring. In graphite, the carbon atoms are sp2 hybridized with bond angles of 120°, which gives graphite a flat geometry.

# Think About It

- Graphite carbon atoms also -bond to each other since they each have an electron in the unhybridized p orbital.

12.84. Collect and Organize

We are to consider whether the structure of the molecule that would result if the C atoms in graphite were replaced by alternating B and N atoms would be planar or puckered (refer to Figure P12.83).

# Analyze

Boron has three valence electrons and nitrogen has five. Boron and nitrogen are each replacing carbon atoms in graphite (Figure P12.83). Each carbon atom had brought four valence electrons to the original structure.

# Solve

In order to pucker the ring, lone pairs would have to be introduced onto the atoms in the structure. Because B and N with eight total valence electrons replace two C atoms, also with eight valence electrons, the ring of BN atoms remains flat.

# Think About It

BN is boron nitride, a very tough, hard, high-temperature ceramic material.

12.85. Collect and Organize

We can use the edge length of the fcc lattice of C60 to calculate the density of buckminsterfullerene and the radius of a C60 molecule.

# Analyze

The mass of the unit cell may be calculated by multiplying the molar mass of C60 (720.66 g/mol) by the four atoms in an fcc unit cell and dividing by Avogadro’s number. We may determine the volume of the unit cell by cubing the edge length (1410 pm). The density is equal to the mass divided by the volume of the unit cell. Using the relationship r = 0.3536, we may calculate the radius of the C60 molecule.

# Solve

(a)

(b) The radius of the C60 molecules is r = 0.3536(1410 pm) = 498.6 pm.

# Think About It

The C60 molecule has a radius that is roughly five to six times that of most ions or atoms, though the density is similar to that observed for the other allotropes of carbon, graphite and diamond.

12.86. Collect and Organize

We can use the radii of C60 and K+ to determine the type of hole the K+ ions are likely to occupy in K3C60. We can also calculate the density of K6C60, which occupies an fcc lattice.

# Analyze

(a) The ratio of nonhost (K+, 138 pm) to host (C60, 498.6 pm) radii may be calculated to determine if K+ will occupy a tetrahedral (rnonhost/rhost = 0.22 – 0.41) or an octahedral hole (rnonhost/rhost = 0.41 – 0.73). The fcc lattice contains four octahedral holes and eight tetrahedral holes, three of which are occupied in K3C60.

(b) The mass of the unit cell may be calculated by multiplying the molar mass of C60 (720.66 g/mol) by the two atoms in a bcc unit cell, dividing by Avogadro’s number, then adding the mass of the six K+ ions. The edge length of the unit cell may be determined using the relationship r = 0.4330. We may determine the volume of the unit cell by cubing the edge length. The density is equal to the mass divided by the volume of the unit cell.

# Solve

(a) The radius ratio for K3C60 is

This ratio fits nicely in the range expected for a guest occupying tetrahedral holes. Three of the eight tetrahedral holes are occupied by K+ ions.

(b)

# Think About It

The density of K6C60 is higher than that of C60 (calculated in Problem 12.85), as we would expect after adding a metal ion.

12.87. Collect and Organize

- Knowing the distance between the phosphorus atoms in its cubic form, we are to calculate the density.

# Analyze

- Density is mass per unit volume. The mass of phosphorus in one unit cell will be the number of atoms of P in one unit cell multiplied by the molar mass of P and divided by Avogadro’s number. The volume of the unit cell is the cube of the length of the side of the unit cell. Density is usually expressed as grams per cubic centimeter (g/cm3), so we have to convert picometers to centimeters.

# Solve

- Mass of phosphorus in one unit cell

- Volume of the unit cell

- Density of cubic phosphorus

# Think About It

- The density of phosphorus in another form would be different. If we measure the density of a crystal of known composition, we may be able to determine what its unit cell looks like.

12.88. Collect and Organize

For the imaginary form of ice nine where the O atoms are ccp, we are to determine which holes the H atoms would occupy.

# Analyze

The ccp (fcc) structure of O atoms will give four atoms per unit cell. This fcc arrangement contains eight tetrahedral holes and four octahedral holes.

# Solve

The ratio of O to H in the ice is 1:2, so the unit cell must contain eight H atoms along with four O atoms. The H atoms must then be small enough to fit into at least some of the tetrahedral holes. If H occupies all of the tetrahedral holes, the 1:2 ratio of O to H is preserved for ice.

# Think About It

By the radius ratio rule

we expect the octahedral holes to be occupied. However, without also placing H into tetrahedral holes, the 1:2 ratio of O to H for the ice could not be preserved.

12.89. Collect and Organize

From a list of properties, we are to identify which describe ceramics and which are associated with metals.

# Analyze

Metallic bonding in metals allows atoms to slip past each other and be easily deformed. Ceramics have either covalent or ionic bonding (or sometimes a mixture of both) that does not allow the atoms to easily slip past each other when stress is applied. Metals have either partially filled valence bands or overlapping valence and conduction bands that allow electrons to flow through the bands. Ceramics, however, have large band gaps between their valence and conduction bands that render them thermally insulative and nonconductive to the flow of electrons.

# Solve

Ductility, electrical and thermal conductivity, and malleability describe metals. Ceramics can be characterized as being electrically and thermally insulative and brittle.

# Think About It

The bonding differences between metals and ceramics account for their very different properties and, therefore, unique applications.

12.90. Collect and Organize

We are to compare the band structure of TiO2 to Ti to account for the difference in electrical properties.

# Analyze

- TiO2 is a ceramic, whereas Ti is a metal.

# Solve

- In ceramic materials like TiO2, the band gap between the valence band and the conduction band is very large and therefore the substance is an electrical insulator. Titanium, however, being a metal and having partially filled d orbitals, has essentially no band gap (similar to Cu in Figure 12.20) and so is an electrical conductor.

# Think About It

- This difference is due to the type of bonding: TiO2 has ionic bonds, and Ti has metallic bonds.

12.91.  Collect and Organize

We are to write the formula for the mineral formed when Mg2+ replaces Al3+ in kaolinite [Al2(Si2O5)(OH)4].

# Analyze

When replacing Al3+ with Mg2+, we must be careful to put in as many Mg2+ as needed to balance the charge of the Al3+ removed. Since we replace two Al3+ ions (6+ charge) we need 3 Mg2+ to balance the charge.

# Solve

Mg3(Si2O5)(OH)4

# Think About It

Several other ions (Fe3+, Be2+, etc.) could replace the Al3+ in kaolinite.

12.92.  Collect and Organize

We are to write the formula of the compound in which Al3+ ions in pyrophyllite [Al4S8O20(OH)4] are replaced by Mg2+ ions.

# Analyze

We have to be careful to maintain charge balance. There are four Al3+ ions in the compound. This gives a 12+ charge for the Mg2+ ions to replace. We therefore need six Mg2+ for the new formula.

# Solve

Mg6S8O20(OH)4

# Think About It

If we replaced the Al3+ with K+, the formula would be K12Si8O20(OH)4.

12.93. Collect and Organize

For the reaction of KAlSi3O8 with water and carbon dioxide, we are asked to determine whether it is a redox reaction and to balance the reaction to give Al2(Si2O5)(OH)4, SiO2, and K2CO3 as products.

# Analyze

In a redox reaction the oxidation state of atoms must change. All species for this reaction contain O2–, K+, Si4+, H+, Al3+, and C4+.

# Solve

2 KAlSi3O8(s)  +  2 H2O  +  CO2(aq)    Al2(Si2O5)(OH)4(s)  +  4 SiO2(s)  +  K2CO3(aq)

Because none of the atoms change oxidation state, this is not a redox reaction.

# Think About It

In this weathering process the larger silicate anion Si3O84– is broken down by water to Si2O52– and SiO2.

12.94.  Collect and Organize

We are to write the balanced equation to describe the conversion of albite (NaAlSi3O8) to jadeite (NaAlSi2O6) and quartz (SiO2).

# Analyze

The difference in the silicate ion portion of the two minerals is SiO2, which is the formula for quartz.

# Solve

NaAlSi3O8(s)  NaAlSi2O6(s)  +  SiO2(s)

# Think About It

Though all of the reactants are solids, this may be classified as a decomposition reaction.

12.95.  Collect and Organize

For the transformation of anorthite (CaAl2Si2O8) to a mixture of grossular [Ca3Al2(SiO4)3], kyanite (Al2SiO5), and quartz (SiO2) under high pressure, we are asked to write the balanced equation and to determine the charges on the silicate anions.

# Analyze

The charge on the silicate ions is found knowing that the cations are Ca2+ and Al3+.

# Solve

(a) 3 CaAl2Si2O8(s)    Ca3Al2(SiO4)3(s)  +  2 Al2SiO5(s)  +  SiO2(s)

(b) In anorthite, the silicate anion is Si2O88–.

In grossular, the silicate anion is SiO44–.

In kyanite, the silicate anion is SiO56–.

# Think About It

There are many silicate minerals in nature.

12.96.  Collect and Organize

We are to balance the equation that produces grossular and calculate gehlenite’s composition as % CaO, 
% Al2O3, and % SiO2.

# Analyze

We can balance the reaction by inspection and then calculate the percentage of CaO, Al2O3, and SiO2 by assuming one mole of gehlenite (Ca2Al2SiO7, molar mass 274.20 g/mol).

# Solve

(a) Unbalanced reaction: CaAl2Si2O8(s)  +  Ca2Al2SiO7(s)  +  CaSiO3(s)    Ca3Al2(SiO4)3(s)

Balancing for Al on the products side gives

CaAl2Si2O8(s)  +  Ca2Al2SiO7(s)  +  CaSiO3(s)    2 Ca3Al2(SiO4)3(s)

Balancing Ca on the reactants side also balances the Si:

CaAl2Si2O8(s)  +  Ca2Al2SiO7(s)  +  3 CaSiO3(s)     2 Ca3Al2(SiO4)3(s)

(b) Gehlenite, Ca2Al2SiO7, can be broken down into 2 CaO + Al2O3 + SiO2. The percent mass of each of these components assuming one mole of gehlenite is

# Think About It

Mineralogists use these kinds of percent composition to simplify comparisons between complex and related minerals.

12.97.  Collect and Organize

Given the radii of Ba2+, Ti4+, and O2– (135, 60.5, and 140 pm, respectively), we can use the radius ratio rule to determine which holes Ba2+ and Ti4+ occupy in a closest-packed arrangement of O2– anions.

# Analyze

The radius ratio can help us predict whether the smaller ion would fit into a cubic (radius ratio 0.73–1.00), octahedral (0.41– 0.73), or tetrahedral (0.22– 0.41) hole in the crystal lattice.

# Solve

Cubic holes can accommodate Ba2+:

Octahedral holes (maybe tetrahedral) can accommodate Ti4+:

# Think About It

Ti4+ has a radius ratio at the edge of the tetrahedral–octahedral ranges, so it is difficult to predict which of these holes it will occupy.

12.98.   Collect and Organize

For LiMnTiO4 we are to determine which metal is expected to occupy the tetrahedral holes of the closest-packed O2– ions.

# Analyze

This metal oxide has a spinel structure that can be generalized as AB2O4 where the total charge on A + 2B = 8+. In this compound the metal ions are Li+, Mn3+, and Ti4+. The radii of these ions are given as 76 pm, 
67 pm, and 60.5 pm, respectively, and the O2– ion has a radius of 140 pm.

# Solve

The ion that is most likely to occupy the tetrahedral holes is the smallest ion, Ti4+.

# Think About It

The radius ratio of Ti4+ to O2– gives a value of 0.432, which is slightly out of the range for occupation of Ti4+ in the tetrahedral holes of the O2– lattice. The radius ratios for Li+ and Mn3+ (0.54 and 0.48, respectively) are much higher and those ions would clearly occupy the octahedral holes in the oxide ion lattice.

12.99.   Collect and Organize

We are asked to explain why an amorphous solid does not give sharp peaks when scanned by X-ray diffraction.

# Analyze

X-ray diffraction gives sharp peaks for crystalline materials that have a regular repeating array of atoms. Amorphous materials have no long-range order in their arrangement of atoms.

# Solve

An amorphous solid has no regular repeating lattice to diffract the X-rays and therefore cannot give rise to the distinct constructive and destructive interference needed to produce sharp peaks in the X-ray diffraction scan.

# Think About It

Amorphous materials in X-ray diffraction either give no signal or may show very broad peaks.

12.100. Collect and Organize

We consider why X-ray diffraction cannot be used for solutions.

# Analyze

X-ray diffraction gives sharp peaks for crystalline materials that have a regular repeating array of atoms.

# Solve

A solution does not have atoms or molecules arranged in a regular repeating lattice to diffract the X-rays. The atoms or molecules are in random orientations and constantly moving.

# Think About It

To obtain a crystal structure, not only must we have a solid, but the solid must also have long-range order of the atoms or molecules. For molecular compounds, this means that we must have a “single crystal” of the compound in which the molecules have all crystallized in the same way with respect to each other.

12.101. Collect and Organize

X-rays and microwaves are both electromagnetic radiation. We are to consider why X-rays, not microwaves, are used for structure determination.

# Analyze

X-rays have wavelengths of the order of 10 to 10,000 pm. Microwaves have wavelengths of the order of 1 mm to 1 m.

# Solve

The separation of atoms in crystal lattices is of the order of 10–10 m, or 100 pm. X-rays have wavelengths of the order of the separation of atoms in crystals, so constructive and destructive interference occurs. Microwaves have wavelengths too long to be diffracted by crystal lattices.

# Think About It

X-ray diffraction is a useful technique, but it has difficulty “seeing” light elements, like H atoms. Complementary information on structure can be obtained from neutron-diffraction experiments.

12.102. Collect and Organize

We are to consider how the wavelength affects an X-ray diffraction pattern.

# Analyze

Diffraction is described by the Bragg equation:

n = 2d sin 

From this equation we see that  and sin  are directly proportional.

# Solve

An increase in  in the Bragg equation would increase sin  and therefore increase . In the pattern shown in Figure P12.102, the peaks would shift to higher 2 values.

# Think About It

Even though we might use a different X-ray wavelength, the values of d we calculate would be the same.

12.103. Collect and Organize

We are to consider why different wavelengths of X-rays might be used to determine crystal structures.

# Analyze

From the Bragg equation

n = 2d sin 

we see that if  is smaller,   is smaller.

# Solve

If a crystallographer uses a shorter  wavelength, the data set can be collected over a smaller scanning range.

# Think About It

In this way the crystallographer can see more data over a smaller scanning range so that if the camera or source can only obtain 2 = 30°, for example, a shorter  would reveal more peaks than a longer .

12.104. Collect and Organize

We are asked to look back to earlier chapters to see where diffraction might have been used to acquire structural information.

# Analyze

As we learned in this chapter, and looking ahead to Chapter 21, X-rays can be used for determining bond distances, for ionizing (putting a charge on) a material, and in imaging.

# Solve

In Chapter 8 (Section 8.8) X-rays were useful in determining the bond lengths listed in Table 8.3.

# Think About It

X-rays in everyday applications help dentists find cavities and doctors diagnose broken bones, cancers, and pneumonia.

12.105. Collect and Organize

Given that the lattice spacing in sylvite (KCl) is larger than in halite (NaCl), we can use the Bragg equation to predict which crystal will diffract X-rays of a particular wavelength through higher 2 values.

# Analyze

Rearranging the Bragg equation to solve for d gives

This shows that sin  is inversely proportional to d.

# Solve

The smaller the distance d (the lattice spacing) the larger the sin  and the larger the 2. Therefore, halite with smaller lattice spacing diffracts X-rays through larger 2 values.

# Think About It

This means that the pattern for NaCl is more spread out than that of KCl.

12.106. Collect and Organize

For the chloride and bromide salts of Ag+, we are to predict which has the greater distance between ion layers and which we would expect to diffract X-rays through larger 2 values.

# Analyze

The size of the atoms or ions making up the lattice determines the spacing between the layers. The greater the atom or ion size, the greater the layer spacing. To determine which lattice diffracts through larger 2 values, we can examine closely the Bragg equation

# Solve

Bromide ions are larger than chloride ions so the distance between AgBr layers is greater than between AgCl layers. Rearranging the Bragg equation to highlight the relationship between  and d gives

From this equation we see that as d (distance between the atom layers) increases, sin  decreases and so 2 will also decrease. The compound expected to diffract X-rays through larger values of 2 is AgCl.

# Think About It

This result might seem counterintuitive. Larger d spacings give lower 2 values.

12.107. Collect and Organize

For galena, which shows reflections in X-ray diffraction ( = 71.2 pm) at 2 = 13.98° and 21.25°, we are asked to determine the value of n for these reflections and to calculate the spacing between the layers of the lattice (d).

# Analyze

To determine n we must find a pattern in the angles of reflection. We notice here that for  = 6.99° and 
 = 10.62° we have a factor of 1.52. The spacing of the layers in the lattice is calculated from the Bragg equation:

# Solve

Because the ratio of the reflection angles () is 10.62°/6.99° = 1.52, the values of n are 2 ( = 6.99°) and 3 
( = 10.62°).

The lattice spacings are

Average lattice spacing (585 + 580)/2 = 582 pm.

# Think About It

The calculated lattice spacings from the reflections may not be exactly equal, but they will be close, as in the example above.

12.108. Collect and Organize

Given that some 2 values for CoO are 42.38°, 65.68°, and 92.60° when  = 154 pm, we are to calculate the n values for these reflections and then the d spacing corresponding to each.

# Analyze

We can use the Bragg equation

We will have to convert the 2 values into . Dividing all the 2 values above by 2 gives  = 21.19°, 32.84°, and 46.30°.

# Solve

To determine n we notice that 32.84° is 1.55 times 21.19° and that 46.30° is 2.18 times 21.19°. The pattern here gives n = 2 (21.19°), n = 3 (32.84°), and n = 4 (46.30°).

The spacings between the layers are

# Think About It

Our assumption about the n values is correct as shown by the single value of d for each n and  combination.

12.109. Collect and Organize

For a lattice distance of 1855 pm, we are to calculate the smallest angle of diffraction (2) for 154 pm wavelength X-rays diffracted in pyrophyllite.

# Analyze

We can rearrange the Bragg equation to solve for sin :

where n = 1 for the smallest angle of diffraction. The 2 value is twice the calculated value of .

# Solve

# Think About It

For n = 3, the reflection would appear at

12.110. Collect and Organize

We can use the Bragg equation:

to determine the smallest angle of diffraction () through minnesotaite when d = 1940  10 pm and  = 154 pm.

# Analyze

The smallest angle of diffraction is when n (the wavelength multiplier) is equal to 1 and when d = 1950 pm.

# Solve

Rearranging the Bragg equation to solve for sin  gives

# Think About It

For n = 2, 3, and 4, the value of  would be 2  2.26°, 3  2.26°, and 4  2.26°.

12.111. Collect and Organize

For a unit cell with X at the eight corners of the cubic unit cell, Y at the center of the cube, and Z at the center of each face, we are to write the formula of the compound.

# Analyze

Each atom at the corner of a cube counts as  in the unit cell. Each atom on a face counts as  in the unit cell. Each atom in the center of the unit cell counts as one.

# Solve

Element X =  8 = 1 X

Element Y = 1  1 = 1 Y

Element Z = 6   = 3 Z

The formula for the compound is XYZ3.

# Think About It

An example of this kind of structure is perovskite, CaTiO3.

12.112. Collect and Organize

Given that a uranium oxide packs into a ccp structure and the oxide ions are located in all of the tetrahedral holes, we are to write the formula for this UxOy salt.

# Analyze

The unit cell for the ccp structure is the face-centered cube. This unit cell would contain four uranium atoms with eight tetrahedral holes.

# Solve

If all of the tetrahedral holes are filled, then there are eight O2– ions in the unit cells. This gives four U and eight O atoms in the unit cell for a formula of UO2.

# Think About It

The oxidation number of uranium in this oxide is +4.

12.113. Collect and Organize

Given the phase diagram for titanium, we can identify the predominant phase under specific conditions and track phase changes as the pressure increases at a constant temperature.

# Analyze

(a) We may identify the phase at 1500 K and 6 GPa by drawing lines from these points along the x and y axes and observing the phase where the lines intersect.

(b) We may track phase changes at a temperature of 725C (998 K) by drawing a vertical line from this point along the x-axis and observing how many phase boundary lines it crosses.

# Solve

(a) At 1500 K and 6 GPa, titanium is present in the bcc () phase.

(b) Titanium undergoes two phase changes as we increase pressure. The transitions are hcp ()  bcc () around 6 GPa, and bcc () hex (3, ) around 11 GPa.

# Think About It

Don’t forget to check the units on your temperature. If you had looked for phase transitions as we increase the pressure at 725 K, you would have discovered only one.

12.114. Collect and Organize

Given the phase diagram for thallium, we may determine the temperature and pressure where all three solid phases (fcc, bcc, and hcp) are present and determine whether the melting point increases, decreases, or stays constant as pressure increases.

# Analyze

The phase boundaries will all intersect where all three solid phases of thallium are present. Drawing horizontal and vertical lines from this point to the axes will allow us to read the temperature and pressure at which these phases are all present. The behavior of the melting point may be determined by following the phase boundary line separating the bcc and liquid phases.

# Solve

(a) All three solid phases of thallium are present at approximately 390 K and 3.8 GPa.

(b) The melting point will increase as the pressure increases (slope is positive).

# Think About It

The positive slope of the solid/liquid phase boundary line indicates that like most species, the density of solid thallium is greater than that of the liquid phase.

12.115. Collect and Organize

We consider cubic nanoparticles of Ag (25 nm on each side) and are asked to calculate the number of unit cells in a particle, the number of Ag atoms in a particle, and the number of silver atoms present in 1360 g of silver nanoparticles.

# Analyze

(a) We are given that the unit cells are body-centered cubic. In this arrangement the unit-cell edge length  is where r is the radius of the silver atom. From the Appendix 3, the radius of a silver atom is 144 pm. Dividing the side length of a nanoparticle by the edge length of the unit cell, we may determine the number of unit cells along an edge of the nanoparticle; we may determine the number of unit cells per particle by cubing this value.

(b) The number of atoms in the nanoparticle may be found by multiplying the number of unit cells per particle, determined in (a), by four Ag particles per bcc unit cell.

(c) Converting the mass of silver to grams, dividing by the molar mass of Ag (107.8682 g/mol), multiplying by Avogadro’s number, and dividing by the ratio of silver atoms per nanoparticle determined in (b) will furnish the number of nanoparticles in a sock.

# Solve

- The edge length of a silver unit cell is

The number of unit cells in a nanoparticle edge is

An edge may not contain a fraction of a unit cell, so we must round down. Cubing this edge length gives (61)3 = 2.3  105 unit cells per particle.

- The number of Ag atoms in a nanoparticle is

- The number of nanoparticles in one sock is

# Think About It

Even though nanoparticles are very small, they still contain thousands of Ag atoms.

12.116. Collect and Organize

Given the dimensions of a gold “nanorod” (a cylinder), we may determine the number of gold atoms in a nanorod, the number of unit cells in a nanorod, and the mass of a nanorod.

# Analyze

Gold crystallizes in an fcc unit cell.

(a) and (b) We may determine the volume of the cylinder (V = r2h) given the diameter (32 nm) and height (67 nm). The volume of the unit cell may be determined using the radius of the gold atom (144 pm) and the relationship r = 0.3536. By cubing the edge length, we may determine the volume of the gold unit cell. Dividing the volume of the nanorod by the volume of the unit cell, we may determine the number of unit cells in a nanorod. In an fcc lattice, there are four atoms in a unit cell, so the number of gold atoms in a nanorod is four times the number of unit cells in a nanorod.

(c) The mass of each nanorod is equal to the number of gold atoms in a nanorod as determined in (a), divided by Avogadro’s number, and multiplied by the molar mass of gold (196.9666 g/mol).

# Solve

- Volume of the nanorod:

Volume of the unit cell

The number of unit cells in a nanorod is

The number of gold atoms in a nanorod is

- There are 7.9  105 unit cells in a gold nanorod.

- The mass of each nanorod is

# Think About It

Although each nanorod is quite small, each one contains nearly one million unit cells!

12.117. Collect and Organize

We consider different possible crystal structures of Fe (radius 126 pm) and compare the densities of bcc and hcp iron and calculate the density of a crystal of 96% Fe and 4% Si.

# Analyze

For each structure, the density is the mass of atoms in the unit cell divided by the volume of the cubic unit cell. For the bcc unit cell there are two atoms per unit cell and the edge length is . For the hcp unit cell there are two atoms per unit cell.

# Solve

(a) The edge length of a bcc unit cell is

The volume of the unit cell is

The mass of the unit cell is

The density is

(b) In the hcp unit cell there are also two atoms in the unit cell. We are given that the volume of the unit cell is 5.414  10–23 cm3, so the density is

(c) If 4% of the mass is due to Si replacing Fe, the molar mass of the alloy would be

The mass of two atoms in the unit cell would be

The density is

# Think About It

Replacing Fe with an element of lower molar mass (silicon) gives a lower density alloy.

12.118. Collect and Organize

For MgSr, which crystallizes in the CsCl bcc structure, we are to calculate the density using the known value of the unit-cell edge length (390 pm).

# Analyze

The bcc structure of MgSr contains one Mg atom and one Sr atom in the unit cell. From that information we can calculate the mass of the unit cell. For the volume of the unit cell, we need only to cube the given edge length.

# Solve

Mass of unit cell

Density

# Think About It

The radii of Mg (160 pm) and Sr (215 pm) are close enough that it is reasonable to think that the Mg atoms would fit well into cubic holes in a lattice of Sr atoms (radius ratio = 0.744, which is just beyond the high end of the octahedral radius ratio range).

12.119. Collect and Organize

For the same crystalline structure of AuZn with  and AgZn with we can use the different molar masses of gold and silver and the length of the unit-cell edges to calculate the densities and predict which alloy is more dense.

# Analyze

Because gold has a much higher molar mass than silver, we can easily predict that the density of the AuZn alloy would be greater than that of the AgZn alloy, despite the slightly smaller unit-cell edge length and therefore smaller volume.

# Solve

For AuZn

For AgZn

The AuZn alloy is more dense than the AgZn alloy.

# Think About It

Indeed, the prediction was correct and AuZn is substantially more dense than AgZn.

12.120. Collect and Organize

By consulting Figure P12.120, we are asked to determine the coordination number of the holes between close-packed layers and to determine if there are other types of holes in this structure.

# Analyze

The close packed layers are stacked directly on top of one another, creating aaaa… layers. It is difficult to see the holes in Figure P12.120, but if we expand the view, separating the layers, it is easier to observe the number of nearest neighbors for each hole

Holes are related in similar fashion to the atoms in a unit cell.

# Solve

From the figure, we see that each hole is directly adjacent to six spheres, so each has a coordination number of 6. All spheres in the unit cell are equivalent, so all holes are equivalent as well.

# Think About It

This is an unusual arrangement of close-packed layers. It is more common to find close-packed layers in an ababab… or abcabc… repeating pattern.

12.121. Collect and Organize

We are asked how Mn would incorporate into an iron lattice, either in the holes or as a substitute for iron.

# Analyze

To occupy holes in the structure, Mn would have to have a distinctly smaller radius than the Fe radius. From Appendix 3, we find that the Mn radius is 127 pm and the Fe radius is 126 pm.

# Solve

The radii of these metals are very similar, so Mn likely forms a substitutional alloy with iron.

# Think About It

The radius of carbon (77 pm) is small enough to fit into the interstices of the iron–manganese lattice. The radius ratio of carbon to iron (77/126) gives a value of 0.61. This indicates that carbon would fit into the octahedral holes of the iron lattice.

12.122. Collect and Organize

In considering alloys with aluminum, we are to decide whether the sizes of the atoms in each alloy indicate that the alloy would be substitutional, not interstitial. Additionally, we are to calculate the density of LiAl if it has a bcc structure.

# Analyze

(a) For an alloy to be substitutional, the two metals should crystallize in the same structures, and the sizes of the metal atoms should be within 15% of each other. For each of the alloys we need to calculate the size ratio of the small atom in the alloy to the large atom in the alloy. If this ratio is 0.85 or greater, then the alloy would be predicted to be substitutional. We are given the radii of the atoms: Al = 143 pm, Li = 
152 pm, Au = 144 pm, and Ti = 147 pm.

(b) To calculate the density of the bcc LiAl alloy, we need to determine first the volume of the cube using the body diagonal to calculate the length of an edge of the unit cell: 4r =  where

4r = 2  rLi (at the center of the cube) + 2  rAl atom (at the corners of the cube)

The volume of the unit cell is . Next we need to calculate the mass of the unit cell. The bcc unit cell contains one atom of Li and one atom of Al. Using the molar masses of Li and Al and Avogadro’s number, we can calculate the mass of the unit cell. Density is mass per volume, usually expressed as grams per cubic centimeter.

# Solve

(a) The alloy ratios are

All of these alloys have atoms within the required 15% size difference of each other, so we certainly would predict that these would be substitutional alloys.

(b) Rearranging the body diagonal equation to solve for  gives:

# Think About It

Aluminum alloys are important for their strength at low temperatures, resistance to corrosion, high electrical conductivity, and ease of being cast into any shape.

12.123. Collect and Organize

From the formula Cu3Al for an alloy with a bcc structure, we are to determine how the copper and aluminum atoms are distributed between the unit cells.

# Analyze

The bcc unit cell contains two atoms. The radii of Al and Cu are 143 and 128, respectively. The radius ratio is 0.895.

# Solve

The radius ratio indicates that Cu atoms fit into the cubic holes of the Al lattice. Another way to look at this is as a simple cubic arrangement of Cu atoms with an Al atom in the center of the unit cell. To be consistent with the formula (Cu3Al), we would have to consider three unit cells, one of which would have one Al atom in the center.

# Think About It

It is probably also possible to have an alloy of formula Al3Cu since their atomic radii are so similar.

12.124. Collect and Organize

We consider the structure of AlP as both an ionic compound and as a covalent compound.

# Analyze

For both types of possible bonding for AlP we can use the radius ratio rule to determine whether the ionic and covalent radii are consistent with the sphalerite structure of AlP. The sphalerite structure has an fcc arrangement of P3–, with Al3+ occupying half of the eight tetrahedral holes. The radius ratio range for tetrahedral holes is 0.22–0.41.

# Solve

(a)

This radius ratio is below 0.41. Yes, the Al3+ would fit into tetrahedral holes to give a sphalerite structure.

(b) The atomic radii from Appendix 3 are 143 pm for Al and 110 pm for P. For a lattice of P atoms,

If we consider the P atoms in a lattice of Al atoms,

Both of these ratios are inconsistent with the size requirements of atoms in a molecular sphalerite structure. No, AlP would not adopt a lattice that corresponds to a covalent compound.

# Think About It

From our calculations, we can say that the bonding in AlP is mostly ionic given that it has a sphalerite structure.

12.125. Collect and Organize

For each description of a reaction, we are to write a balanced chemical equation.

# Analyze

We first have to write the chemical formulas of the named reactants and then complete and balance the equations.

# Solve

(a)	SiO2(s)  +  C(s)    CO2(g)  +  Si(s)

(b)	Si(s)  +  2  Cl2(g)    SiCl4

(c)	Ge(g)  +  2  Br2    GeBr4(s)

# Think About It

All of these are redox reactions in which a group 14 element is either oxidized (b and c) or reduced (a).

12.126. Collect and Organize

For the reactions of Sn with Cl2, Pb with Cl2, and for the thermal decomposition of SiCl4, we are asked to write balanced chemical reactions.

# Analyze

In the balanced equations we should include the physical state of the reactants and products. In the reaction of gaseous Cl2 with solid Sn or Pb, we form liquid SnCl4 and solid PbCl2, respectively. In the thermal decomposition of liquid SiCl4, we form solid Si and gaseous Cl2.

# Solve

- Sn(s)  +  2 Cl2(g)    SnCl4

- Pb(s)  +  Cl2(g)    PbCl2(s)

- SiCl4Si(s)  +  2 Cl2(g)

# Think About It

Lead might also form PbCl4 which would require 2 moles of Cl2 for every mole of Pb in the balanced chemical equation.

12.127. Collect and Organize

We can use the Bragg equation

to solve for the distance between the layers of silicon in CaSi2 given 2 values of 29.86° (n = 2), 45.46° (n = 3), and 62.00° (n = 4) when 154 pm X-rays are diffracted through a crystal. We are then to compute the distance between Ca2+ and a silicon layer, knowing that the calcium ions are located halfway between the layers. Lastly, we are to consider how CaSi2 could act as a “deoxidizer.”

# Analyze

(a) To find the distance between the silicon layers we need to rearrange the Bragg equation to solve for d, the distance between diffraction planes or the distance between planes of silicon atoms in the structure.

We will compute the d value using all three 2 values, but they should yield the same value.

(b) To find the distance between Ca2+ ions and a layer of silicon atoms, we need only divide the d spacing from part a by 2.

(c) From the name “deoxidizer” and the oxidation state of –1 of the Si atoms in CaSi2, we can infer that the Si atoms in the calcium silicide will act as reducing agent being themselves oxidized to Si4+, the most common oxidation state for silicon.

# Solve

(a)	For 2 = 29.86°,  = 14.93°

For 2 = 45.46°,  = 22.73°

For 2 = 62.00°,  = 31.00°

The distance between the Si layers is 598 pm.

(b)	The Ca–Si distance is d/2 = 598 pm/2 = 299 pm.

(c)	In deoxidizing the iron, silicon is oxidized to Si4+ and any iron cations (such as Fe3+) are reduced to Fe.

# Think About It

The calcium ion, Ca2+, has an ionic radius of 100 pm, so it fits well into the layers of Si atoms, which are nearly 600 pm apart.

12.128. Collect and Organize

We consider how the “average” value of the ionization energies and electron affinities of group 14 elements like C, Si, Ge, and Sn explains their tendency to form covalent bonds rather than ionic bonds.

# Analyze

Ionization energy is the energy required (usually endothermic) to remove an electron from a gaseous species. Electron affinity is the energy change (may be endothermic or exothermic) when a species gains an electron.

# Solve

Group 14 elements do not have low ionization energies or electron affinities, so they tend to neither easily lose nor easily gain an electron. As a result, they form bonds by sharing electrons, not by giving up or accepting electrons.

# Think About It

Two of these elements (Si, Ge) are also quite good as semiconductors whose band gap is intermediate between metals and insulators.